LIQUIDS         DENSITY	 Boiling Pt.        FLAMMABLE         ODOR                  DISSOLVES

(g/cm3)	    (0C)						                   SUGAR

Water             		 1.00                   100                 	no	        	    none	            	 yes

Ethanol         		 0.82                     78	               	yes	        	   strong            	 no

# Methanol       		 0.79                     65	               	yes	        	   slight sweet	            no

# Isopropyl	0.83	81	yes	strong 	no

SOLUBLE  SALTS                          Flame Test           	     SOLUBLE  SALTS                	Flame Test

Sodium Chloride               	yellow/orange	Lithium Chloride	Red/Fusha

Potassium Chloride	purple/pink                         	Copper Chloride	Blue/Green

Cobalt Chloride	Sparkling silver	Borax	Yellow

INSOLUBLE  POWDERS               Acid Test

Calcium Carbonate				Yes

Calcium Fluoride				No

INSOLUBLE SOLID      REACTS WITH	       DENSITY          COLOR    	 ADDITIONAL INFORMATION

ACID                        (g/cm3)

Metals

Lead					no                        	11.3		black		Very soft, leaves dark streak on paper, not magnetic,

will not rust in water

Copper					no			  8.9		orange		Can be scratched with metal, not magnetic, malleable,

will not rust, will turn a flame green if heated 30 seconds.

Iron					slightly		  7.9		black/silver	Rust in contact with water, magnetic

Tin					no			  7.3		shiny silver	Not magnetic, malleable, shiny, will not rust.

Zinc					slightly		  7.1		dull silver	Not magnetic, becomes dull, malleable,

will not rust in water

Aluminum				slightly		  2.7		silver		Not magnetic, malleable, will not rust in water

# Steel	slightly	7.6	silver	Metal alloy, magnetic, malleable, shiny, rusts in water

INSOLUBLE SOLID      REACTS WITH	       DENSITY          COLOR    	 ADDITIONAL INFORMATION

ACID                        (g/cm3)

Silicon	no	2.3	shiny gray	Metalloid, will not rust in water, not magnetic,

Glass					no			  2.3		clear		Melts at only high temps, scratches glass.

# Plastic					no		         0.5 -   1.4	varies		Slightly flammable, will not scratch glass, melts

# PETE		1.3-1.4		Soda & Water containers, waterproof packages

# HDPE		0.95		Milk, detergent & oil bottles, toys and plastic bags.

# PVC		1.39-1.42		Water pipes, hard, rigid, white in color usually.

# LDPE		0.92		Many plastic bags, shrink wrap, garment bags

# PP		0.90-0.92		Refrigerated containers, some bags, most bottle tops.

# PS		1.04-1.10		Throwaway utensils, meat packing, protective packing.

# Acrylic		1.16-1.19		Appears like glass.

Wax					no			  0.85		varies		Usually floats in water and sinks in alcohol, melts,

will not scratch glass, marks paper.

Pumice					no			  0.85		whitish		Usually floats in water, won't melt.

# Quartz chips	no	2.65	varies	Can be in crystal form, also found in granite rock

# Limestone or limestone chips	yes	1.1 - 3	gray – white	Made from living organisms like sea shells and coral , density varies on how the limestone rock was formed

Rock					no			varies		varies		Name as :Igneous , metamorphic, sedimentary.  Use references!

Seeds 					no			varies		varies		Specific Names: Pop corn, black beans, pinto beans, corn,

peas- research is required to figure out appropriate name.

Wood (Popular, oak, pine, cork)	no			0.35-0.9	varies		See chart in classroom for exact name, or internet.

Silicone/Rubber			no			0.968-2.8	varies		Silcone is white and soft, easy to bend. Rubber is harder

and bounces when dropped